## Slide 1: Off-lattice kinetic Monte Carlo and hydrogen vacancy-cluster interactions in α–Fe
C.J. Williams
University of Cambridge
Enrique Galindo-Nava – University College London
James Elliott – University of Cambridge
Notes: Enter speaker notes here.

## Slide 2: Outline
Motivation & intro to off-lattice KMC (OLKMC)
Accelerating OLKMC
  Local environments, tolerant classification.
  Self symmetries.
  An adaptive catalogue.
Results
  Vacancy clusters, H-complexes and lifetimes
Notes: Enter speaker notes here.

## Slide 3: H-embrittlement
CC
DFT
MD
CM
mm
μm
nm
fs
ps
ns
μs
ms
s
H-embrittlement
Notes: Micrograph relevant – Martensitic steal
DFT vs kinetics and large scale
PLOT time vs length scales
Composition, cast iron
Microstructure
Energy separations
Hydrogen embrittlement time-scales – (seconds) + length scales
High mobility
Unknown mechanisms (defect interactions)
Difficult experimentally (electron density)
Micrograph relevant – Martensitic steal
DFT vs kinetics and large scale
PLOT time vs length scales
Composition, cast iron
Microstructure
Energy separations
Hydrogen embrittlement time-scales – 𝑂(seconds) + length scales
High mobility
Unknown mechanisms (defect interactions)
Difficult experimentally (electron density)

## Slide 4: H-embrittlement
CC
DFT
MD
CM
mm
μm
nm
fs
ps
ns
μs
ms
s
H-embrittlement
Notes: Micrograph relevant – Martensitic steal
DFT vs kinetics and large scale
PLOT time vs length scales
Composition, cast iron
Microstructure
Energy separations
Hydrogen embrittlement time-scales – (seconds) + length scales
High mobility
Unknown mechanisms (defect interactions)
Difficult experimentally (electron density)
Micrograph relevant – Martensitic steal
DFT vs kinetics and large scale
PLOT time vs length scales
Composition, cast iron
Microstructure
Energy separations
Hydrogen embrittlement time-scales – 𝑂(seconds) + length scales
High mobility
Unknown mechanisms (defect interactions)
Difficult experimentally (electron density)

## Slide 5: (Kinetic) Monte Carlo
Markov chain through state-space
Harmonic approximation to TST:
Notes: Much faster than MD – order seconds for some systems
Construct lattice such that states correspond to basins/minima of MD’s PE

## Slide 6
Notes: Energy landscape in continuous picture

## Slide 7
Notes: Reference Moleclar dynamics

## Slide 8
Notes: What we want for fast (K)MC

## Slide 9
Notes: Saddle points are key – describe discrete possible transitions

## Slide 10
Notes: Saddle points are key – describe discrete possible transitions
htst

## Slide 11: Off-lattice KMC
KMC
choose
mechanism
Find
saddle
points
Advance
state
Notes: Lead into find saddle points as the slow point and that this needs to be done efficiently
  Kinetics, on-the-fly, arbitrary, basin-escaping.
  Completeness, force-field.

## Slide 12: Outline
Motivation & intro to off-lattice KMC (OLKMC)
Accelerating OLKMC
  Local environments, tolerant classification.
  Self symmetries.
  An adaptive catalogue.
Results
  Vacancy clusters, H-complexes and lifetimes
Notes: How symmetry lest a SPS go further

## Slide 13: Locality
Notes: Reduce SPS in frame
Store, reduce SPS between frames

## Slide 14: Local environments
Notes: Reduce SPS in frame
Store, reduce SPS between frames

## Slide 15: Equivalence?
Notes: Tolerance requires a continuous heuristic

## Slide 16: Invariant and tolerant equivalence

## Slide 17: Invariant and tolerant equivalence

## Slide 18: Invariant and tolerant equivalence

## Slide 19: Invariant and tolerant equivalence

## Slide 20: Invariant and tolerant equivalence

## Slide 21: Invariant and tolerant equivalence
Notes: Make connection to energy
Bad exponential complexity: exploit embedding space O(n^2) => could be O(n)
How to set delta:

## Slide 22: Invariant and tolerant equivalence
Notes: Make connection to energy
Bad exponential complexity: exploit embedding space O(n^2) => could be O(n)
How to set delta:

## Slide 23: Efficiency
Notes: N = 430ish
RHS = V1 H

## Slide 24: Internal symmetries
*
Notes: Use the same tolerance for equivalence and self symmetries

## Slide 25: Adaptive

## Slide 26: Adaptive

## Slide 27: Adaptive
Find:
Generate:

## Slide 28: Adaptive
Find:
Generate:
Test

## Slide 29: Outline
Motivation & intro to off-lattice KMC (OLKMC)
Accelerating OLKMC
  Local environments, tolerant classification.
  Self symmetries.
  An adaptive catalogue.
Results
  Vacancy clusters, H-complexes and lifetimes
Notes: Enter speaker notes here.

## Slide 33
Notes: Effect of H vs H free case

## Slide 34
Notes: Effect of H vs H free case

## Slide 35
Diffusivit
Notes: Graph
Vacancies
Diffuse

## Slide 37: *preliminary
Complex |  | with H |  | with H
Complex |  |  |  | 

## Slide 38: Summary
Tolerant, invariant and continuous equivalence
Adaptive catalogue
Classified complexes’ diffusion pathways
Hydrogen can lower diffusion barrier
H de-trapping barrier(s) from clusters
H effective diffusivity
Quantified the trapping atmospheres surrounding vacancy clusters
Cluster lifetimes
Notes: Take away
PAPER LINK

## Slide 39: Try openFLY - github.com/ConorWilliams/openFLY
Fully documented
Parallelised
Open source
Implements all discussed and more (graph based methods, etc)
Supports the GSD format
Supports openKIM (EAM, DUNN, EMT, EDIP, MEAM, hNN, LJ_*, Tersoff, …)
Notes: Enter speaker notes here.
MOVE UP

## Slide 40: Acknowledgements
We gratefully acknowledge the funding received from the EP-SRC via the CDT in Computational Methods for Materials Science (Grant number EP/L015552/1) and grant EP/T008687/2.
E. I. Galindo-Nava acknowledges the Royal Academy of Engineering for his research fellowship funding.
We also acknowledge Rolls-Royce PLC for the provision of funding. All information and foreground intellectual property generated by this research work is the property of Rolls-Royce PLC.
Notes: Enter speaker notes here.

## Slide 41: Complex diffusion
Notes: Graph

## Slide 42: H parameters

## Slide 44: Symmetries and local environments
Euclidean
invariants
Notes: Intra atomic
Euclidean

## Slide 45: Topological representation
Adjacency
Notes: Numbers
Adjacency matrix
Test for graph isomorphisms

## Slide 46: Topological representation - problems
Notes: Also not sensitive to small changes in structure, i.e induced by small H movements

## Slide 47: Topological representation - problems
Notes: Also not sensitive to small changes in structure, i.e induced by small H movements

## Slide 48: Topological representation - problems
Notes: Also not sensitive to small changes in structure, i.e induced by small H movements

## Slide 49: Topological representation - problems
Notes: Also not sensitive to small changes in structure, i.e induced by small H movements

## Slide 50: Topological representation - problems
Notes: Also not sensitive to small changes in structure, i.e induced by small H movements

## Slide 51
Notes: Explain dimer method – invert component of force parallel to min eigenmode
Discovers mechanisms without any input or hints
PAPER
Summary: find SP; compute rates using HTST; choose mech (KMC); progress time (KMC)

## Slide 52: Hierarchical catalogue

## Slide 53: Hierarchical catalogue

## Slide 54: Hierarchical catalogue

## Slide 55: Hierarchical catalogue
Notes: RM acronyms simpliy
Same size

## Slide 56: Invariant and tolerant equivalence

## Slide 57: Greedy algorithm

## Slide 58: Greedy algorithm

## Slide 59: Greedy algorithm

## Slide 60: Greedy algorithm

## Slide 61: Exponential?

## Slide 62: Exponential?

## Slide 63: Rotation
Given permutation that satisfies equivalence
Orthogonal Procrustes problem:
Solution via SVD
s.t.

## Slide 64: Adaptive catalogue

## Slide 65: Adaptive catalogue

## Slide 66: Adaptive catalogue

## Slide 67: Adaptive catalogue
Test

## Slide 68: The flickering problem
Notes: Particular problem in Fe-H system as Tet->Tet H transition energy barrier order of magnitude lower energy barrier

## Slide 69: Superbasins
Partition mechanisms into transient and absorbing:
Notes: Build Superbasins on the fly
Compute mean residence time in basin (matrix transformation)